## Slide 1: Topological Insulators(TI)
1
Hasan and Kane, Rev. Mod. Phys. 82, 3045 (2010).
Qi and Zhang, Rev. Mod. Phys. 83, 1057 (2011).
Band Insulator
Conduction Band
Valence Band
Strong Spin Orbit Coupling
Topological Insulator
Conduction Band
Valence Band
Conduction Band
Valence Band
Edge State/
Surface States

## Slide 2: Theoretical Prediction and Realization of TI
2D TI (QSH insulator)
HgTe quantum wells
InAs/GaSb quantum wells
Bernevig et al., Science 314, 1757 (2006).
König et al., Science 318, 766 (2007).
Liu et al., Phys. Rev. Lett. 100, 236601 (2008).
Knez et al., Phys. Rev. Lett. 107, 136603 (2011).
3D TI
BixSb1-x alloys
Fu & Kane, Phys. Rev. B 76, 045302 (2007).
Hsieh et al., Nature 452, 970 (2008).
Zhang et al., Nat. Phys. 5, 438 (2009).
Xia et al., Nat. Phys. 5, 398 (2009).
Chen et al., Science 325, 178 (2009).
1T’ monolayer WTe2
Fei et al., Nat. Phys. 13, 677 (2017).
Tang et al., Nat. Phys. 13, 683 (2017).
Wu et al., Science 359, 76 (2018).
Bi2Se3 family

## Slide 3: Photoelectric Effect
Ekin=hf – Eb – Φ
Heinrich Hertz
Albert Einstein
"for his services to Theoretical Physics, and especially for his discovery of the law of the photoelectric effect"

## Slide 4: Angle-resolved photoemission spectroscopy(ARPES)

## Slide 5: The Dirac SS in Bi2Se3 family
Bi2Te3
Bi2Se3
Dirac surface states of 3D TIs are observed in ARPES.
Y. L. Chen et al., Science 325, 178 (2009)
D. Hsieh et al., Nature 460, 1101 (2009)

## Slide 6: Molecular Beam Epitaxy (MBE)
Slow growth rate (0.2nm/min)
Ultra-high vacuum (10^-10 mbar)
Thickness/interface engineering

## Slide 7: Crossover from 2D to 3D of Bi2Se3
Zhang, Y., He, K., Chang, CZ. et al. Nature Phys 6, 584–588 (2010).

## Slide 8: Scanning Tunneling Microscope
Tunneling current depends on tip-sample distance.
Fixing current -> fixing tip-sample distance -> Tip reads surface morphology

## Slide 9: Scanning Tunneling Spectroscopy (STS)
I is continuous recorded with changing voltage bias.
Differential conductance (dI/dV) resolves local density of states

## Slide 10: Landau quantization in Sb2Te3
Landau levels are revealed in the STM/S measurements under high B field.

## Slide 11: Landau quantization in Bi2Se3
Xue group
Bi2Se3 film
PRL 105, 076801 (2010)
Sasagawa group
Bi2Se3 crystal
PRB 82, 081305R 2010

## Slide 12
(i) Inverted band structure
(ii) Ferromagnetic insulator
Conditions of QAH effect
+ Ferromagnetic order
Conduction Band
EF
Valence Band
Conduction Band
Valence Band
Topological Insulator
Inverted band structure

## Slide 13
Magnetic exchange gap in Fe-doped Bi2Se3
Y. L. Chen et al. Science, 329,659-662(2010)

## Slide 14
C.Z Chang, et al. Phys. Rev. Lett., 112.5 (2014): 056801.
Magnetic exchange gap in Cr-doped Bi2Se3
Magnetic exchange gap observed in both Fe and Cr-doped Bi2Se3.
No long range FM order is observed.

## Slide 15
Zhang, J., Chang, CZ., Zhang, Z. et al. Nat Commun 2, 574 (2011)

## Slide 16: Band engineering of (Bi1-xSbx)2Te3
Zhang, J., Chang, CZ., Zhang, Z. et al. Nat Commun 2, 574 (2011)

## Slide 17: Long-range FM order and Giant AHE in Cr-doped (Bi1-xSbx)2Te3
C.Z. Chang, et al., Adv. Mater., 25: 1065-1070.
Long range FM order is achieved in Cr-doped (Bi1-xSbx)2Te3 .

## Slide 18
QAH effect in Cr-doped TI films
Chang et al., Science 340,167 (2013)
QAH effect with Chern number C = 1
5QL Cr0.15 (Bi0.1Sb0.9)1.85Te3 film

## Slide 19
Chang et al., J. Phys. Condens. Mater. 28, 123002 (2016)
m0H
ryx
Intrinsic AHE: induced by energy band
QAHE
Karplus et al., Phys. Rev. 95,1154 (1954)
From Anomalous Hall effect (AHE) to QAH effect
m0H
ryx